## Slide 1: Part 2: WSDOT’s Bridge Deck Preservation Program

## Slide 2
Washington State Map
Eastern Washington
Western Washington
Notes: Washington State has three distinctive areas, Eastern, Western Washington and the Cascade Mountains.

## Slide 3
Chart: 
| Concrete | Prestress Conc | Steel | Timber
Deck Area | 15599527 | 18660284 | 10541858 | 244867
Nearly 90% of WSDOT bridges built in the past 10 years
are precast prestressed/post-tensioned concrete
% based on bridge deck area
Washington State’s Bridge System
Superstructure Types
Chart: 
| Cast-in-place Conc | Integral w/Beam
Deck Area | 50599826 | 362497
Deck Types
Integral
Non-Integral
2,964
60
3,132 bridges (53.5 M SF)
Repl value $58 Billion
Ave Age - 48

## Slide 4
Chart: 
| Fair | Poor | Good
Deck Area | 17520876 | 1806934 | 26278454
Fair
807 brgs
17.5M SF
Good
2,110 brgs
26.3M SF
Poor
107 brgs
1.8M SF
38.4%
57.7%
3,024 WSDOT Bridges with Conc Deck
WSDOT Conc Bridge Deck Condition
$180M to Repair/overlay

## Slide 5
Steel Truss
Steel Arch
Prestress Girder
WSDOT Concrete Bridge Decks (non-Integral)
Steel Arch
Concrete Arch
Steel Girder
Notes: 3

## Slide 6
WSDOT Concrete Bridge Decks (Integral)
Floating
Bridge
Segmental Post-Tension Box
Prestress Bulb-T
Conc Box
Precast Prestress Slab
Conc T-Beam
Notes: 3

## Slide 7
Concrete Bridge Deck
Concrete Bridge Deck issues:
Deterioration /Rebar Corrosion
Rutting
Rebar Cover
Poor Quality Concrete
Typical Concrete Bridge Deck
Notes: 3

## Slide 8
1.) salt & water penetrates concrete
2.) rebar corrodes & expands
3.) cracks form causing delams
Deterioration / Rebar Corrosion
Typical Concrete Bridge Deck
Notes: 3

## Slide 9
Typical Concrete Bridge Deck
Deterioration / Rebar Corrosion

## Slide 10
US2 Geiger Blvd OC
Spokane, Wa
Rutting
Prestress Conc Girder
Deck – 5.75”
Year Built – 1964 (54yrs)
Conc Overlay – 1987 (31yrs)
Typical Concrete Bridge Deck
WSDOT Maintenance crews
Applied urethane to wheel ruts in 2017

## Slide 11
Rutting
US2 Geiger Blvd OC
Spokane, Wa
Typical Concrete Bridge Deck

## Slide 12
The only states that explicitly prohibit studded tires for residents year round are Hawaii, Minnesota, Mississippi and Wisconsin.

## Slide 13
Br 99/540 Alaskan Way Viaduct
Rebar Cover
Typical Concrete Bridge Deck

## Slide 14
Poor Quality Concrete
SR10 Bristol Fill
Near Cle Elum
Built in 1937
(Deck Replaced in 2012)
Typical Concrete Bridge Deck

## Slide 15: WSDOT’s Deck Evaluation Process
Inspect and Rate Deck Condition

## Slide 16
WSDOT Bridge Deck BMS Inspection

## Slide 17
WSDOT Bridge Deck BMS Inspection
Condition State 1
The deck surface has no spalls/delaminations or previous repairs. May have cracking or rutting.
Condition State 2
The deck surface has previous repairs.
Condition State 3
The deck surface has spalling.
Condition State 4
Delamination Test Results.
Elem | Description | Total | Unit | State1 | State2 | State3 | State4
12 | Conc. Deck | 3,990 | SF | 2,774 | 1,053 | 0 | 163
35 | Soffit | 3,990 | SF | 3,990 | 0 | 0 | 0
376 | Delam Testing | 3,990 | SF | 3,827 | 0 | 0 | 163
(4%)
90/316N Paha Rd OC - milepost 215.24
Delam Test - October 2001
2012
Year Built – 1972 (46 yrs)
Deck Thickness – 7”
CS2- Patching (26%)

## Slide 18: WSDOT Concrete Deck Evaluation/Rating
Good
Fair
Poor
BMS Condition
(Top of Deck)
NBI Deck Code

## Slide 19
90/316N Paha Rd OC - milepost 215.24
Modified Concrete Overlay
Applied 2013
WSDOT Bridge Deck BMS Inspection
Elem | Description | Total | Unit | State1 | State2 | State3 | State4
12 | Conc. Deck | 3,990 | SF | 2,774 | 0 | 0 | 0
35 | Soffit | 3,990 | SF | 3,990 | 0 | 0 | 0
376 | Delam Testing | 3,990 | SF | 3,827 | 0 | 0 | 0
Good Condition
2012
Poor Condition
90/316N Paha Rd OC

## Slide 20
Good
Fair
Poor

## Slide 21
WSDOT Concrete Deck – 10 yr Preservation Needs
> 5%
2% - 5%
1% - 2%
Overlay 30+ yrs

## Slide 23
2018 Planned Construction
14 bridges (225,175 SF)
WSDOT Concrete Deck Rehab – 2018
SR128 Snake R
128/10 - C9201
Mod Conc – 46,400SF
I-90 3rd Ave OC
290/1W-W – C9264
4,000D – 19,684 SF
I-90 2nd Ave OC
290/2W-W – C9264
4,000D – 6,346SF
US97 Okanogan R
97/534 – C9279
Mod Conc - 11,704SF
I-90 Yakima R
90/154N & S – C9214
4,000D - 35,700SF
I-90 Yakima R
90/140N & S – C9214
4,000D – 23,400SF
US195
195/52 & 60 - C9204
4,000D – 28,720SF
US195 RR OC
195/34 - C9204
4,000D – 6,080SF
US195
195/46 & 49 - C9204
4,000D – 19,685SF
I-90 Winery Rd
90/80S – C9213
Mod Conc - 7,020SF
I-90 Raging River
90/77N – C9213
Mod Conc – 20,436SF

## Slide 24
2019 Planned Construction
5 bridges (55,665 SF)
WSDOT Concrete Deck Rehab – 2019
I-90 Cle Elum R
90/134N & S – Jan 2019
4,000D – 17,582SF
SR18 Holder Cr
18/31N – Oct 2018
4,000D – 12,251SF
SR302 Purdy Br
302/105 – Oct 2018
Polyester – 11,000SF
I-5 Toutle R
5/140W – Apr 2018
Polyester – 14,832SF

## Slide 25
Bridge Deck Repair by WSDOT Maintenance Forces
WSDOT Concrete Deck – 10 yr Preservation Needs

## Slide 26
With constrained Funding for Deck Rehab
This is the new “Normal”
WSDOT Concrete Deck – 10 yr Preservation Needs

## Slide 27
Chart: 
| Bare Conc | Bare Conc-ECR | Conc Overlays | Asphalt | Polyester | Polymer
Deck Area | 8845361 | 13219991 | 13278192 | 8521431 | 742661 | 388783
 | 816351


(19.3%)
(28.9%)
(1.6%)
(30.8%)
(18.6%)
(0.8%)
792
589
564
23
1030
21
Washington State’s Concrete Bridge Deck Program
21
3,039 Bridges with Concrete Decks
45.8 million SF deck area
(2nd and 3rd Gen)
8.8M SF
13.2M SF
14M SF
8.5M SF
Built prior to 1980

## Slide 28
Chart: 
| Fair | Good | Poor
Deck Area | 5283780 | 2497055 | 1055706
286 Bridges
5.3 M SF
(59.8%)
Fair
Good
Poor
43 Bridges
1.0 M SF
(11.9%)
259 Bridges
2.5 M SF
(28.3%)
Ave Age – 53yrs
Oldest – 95yrs
25 bridges
> 75 yrs
589 Bridges
8.8 M SF
WSDOT Bare Concrete Decks

## Slide 29
WSDOT Bare Concrete Decks
Year Built – 1923 (95 yrs)
Deck Thickness – 10”
Width 20 feet
SR155 – Okanogan River
Located in Omak
ADT – 6,884 / day
NBI Deck – 6
“Fair” Condition

## Slide 30
Chart: 
| Bare Conc | Bare Conc-ECR | Conc Overlays | Asphalt | Polyester | Polymer
Deck Area | 8845361 | 13219991 | 13278192 | 8521431 | 742661 | 388783
 | 816351


(19.3%)
(28.9%)
(1.6%)
(30.8%)
(18.6%)
(0.8%)
792
589
564
23
1030
21
Washington State’s Concrete Bridge Deck Program
21
3,039 Bridges with Concrete Decks
45.8 million SF deck area
(2nd and 3rd Gen)
8.8M SF
13.2M SF
14M SF
8.5M SF
Built after
1980

## Slide 31
Concrete Decks with Epoxy Coated Rebar
1910 - 80
1980 - 2007
Uncoated
Rebar
Top Mat
Coated
2007 - present
Both Mats
Coated
792 Bridges
13.2 M SF
Concrete Decks with Epoxy Coated Rebar

## Slide 32
Ave Age – 22yrs
Oldest – 39yrs
Chart: 
| Fair | Good
Deck Area | 2216498 | 11147973
792 Bridges
13.2 M SF
84 Bridges
2.2 M SF
(16.6%)
Fair
Good
709 Bridges
11.0 M SF
(83.3%)
Concrete Decks with Epoxy Coated Rebar

## Slide 33
Prestress Girder Bridge
Year Built – 1979 (39 yrs)
Deck Thickness – 7”
2” Cover – Top Mat
SR22 – Yakima River Overflow
Located near Toppenish, Wa
271 SF Patching and spalls
(0.9%)
NBI Deck – 6
“Fair” Condition
Concrete Decks with Epoxy Coated Rebar
First Generation ECR

## Slide 34
SR303 Manette Bridge (Bremerton, Wa)
Built in 2011
Length – 1,550’ (Max span of 250’)
Concrete Decks with Epoxy Coated Rebar

## Slide 35
SR303 Manette Bridge (Bremerton, Wa)

## Slide 36
SR303 Manette Bridge (Bremerton, Wa)
Built in 2011
Problem - WSDOT has observed abnormal cracking in many concrete bridge decks built between 2000 - 2013

## Slide 37
SR303 Manette Bridge (Bremerton, Wa)
Built in 2011
Problem - WSDOT has observed abnormal cracking in many concrete bridge decks built between 2000 - 2013

## Slide 38
Maintenance Deck Seal trial section - 2016
Cost to seal entire deck about $200,000
Completed in 2018
SR303 Manette Bridge (Bremerton, Wa)

## Slide 39
Chart: 
| Bare Conc | Bare Conc-ECR | Conc Overlays | Asphalt | Polyester | Polymer
Deck Area | 8845361 | 13219991 | 13278192 | 8521431 | 742661 | 388783
 | 816351


(19.3%)
(28.9%)
(1.6%)
(30.8%)
(18.6%)
(0.8%)
792
589
564
23
1030
21
Washington State’s Concrete Bridge Deck Program
21
3,039 Bridges with Concrete Decks
45.8 million SF deck area
(2nd and 3rd Gen)
8.8M SF
13.2M SF
14M SF
8.5M SF

## Slide 40
Chart: Deck Area
| 1979 | 1980 | 1981 | 1982 | 1983 | 1984 | 1985 | 1986 | 1987 | 1988 | 1989 | 1990 | 1991 | 1992 | 1993 | 1994 | 1995 | 1996 | 1997 | 1998 | 1999 | 2000 | 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010
 | 1979 | 1980 | 1981 | 1982 | 1983 | 1984 | 1985 | 1986 | 1987 | 1988 | 1989 | 1990 | 1991 | 1992 | 1993 | 1994 | 1995 | 1996 | 1997 | 1998 | 1999 | 2000 | 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010
 | 13186 | 0 | 61261 | 164558 | 187026 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 1
 | 112981 | 269382 | 145531 | 10752 | 104070 | 570847 | 2292149 | 415361 | 476817 | 1280841 | 1424179 | 531574 | 447630 | 273627 | 205193 | 14653 | 64489 | 56445 | 8700 | 13056 | 21082 | 0 | 20620 | 3120 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 14760 | 15964 | 27960 | 6120 | 205892 | 217181 | 770001 | 74341 | 647790 | 534596 | 489776 | 168669 | 217618 | 83254 | 26098 | 40766 | 129038
 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 6804 | 0 | 23370 | 2816 | 0 | 60840 | 183916 | 68768 | 52583 | 18235 | 24046 | 567640 | 14896 | 35226 | 59387
RSLMC | 3120 | 58310 | 3762 | 8446 | 18174
Latex
Low Slump
Microsilica
Fly-Ash
Rapid Set
LMC
1979
1983
1st Mod
Conc Overlay
Low Slump
Discontinued
2007 - present
1987
1st Microsilica
Conc Overlay
1995
1st Fly-Ash
Conc Overlay
Rapid Set
Discontinued
2002-10
1st Perf Mix Design
Conc Overlay
2016
Bridges with a Modified Concrete Overlay

## Slide 41: Modified Concrete Overlays
Choose between Latex/Microsilica/FlyAsh
Hydromill deck preparation
Overlay Concrete has typical 42hr cure
Diamond grind grooves
Performance mix (2nd generation)
7 day cure
Diamond grind grooves
Section 6-09
Special Provision

## Slide 42: Modified Concrete Overlays
Ave Age – 26yrs
Oldest – 39yrs
187 bridges
(4.9M SF)
> 30 yrs
584 Bridges
14.1M SF
Chart: 
| Fair | Good | Poor
Deck Area | 6985675 | 6484091 | 624777
183 Bridges
7.0M SF
(49.6%)
Fair
Good
357 Bridges
6.5M SF
(46%)
44 Bridges
0.6M SF
(4.4%)
Expected Service Life
25 – 30 years
Total Project Cost
$80 - $100 / SF

## Slide 43: Modified Concrete Overlays
WSDOT 1st Mod Conc Overlay
US2 Pine Creek
1979
“Good” Condition

## Slide 44: Modified Concrete Overlays
WSDOT 1st Mod Conc Overlay
US2 Pine Creek
Yr Built – 1949 (69yrs)

## Slide 45: Modified Concrete Overlays
I-90 Denny Creek Bridge
Segmental Post-Tension Box
Standard rebar in Deck
Year Built – 1980 (38yrs)
LMC Overlay – 1980 (38yrs)
Deck – 10”
Length – 3,620 feet
Width – 52 feet
Repl Value - $200M

## Slide 46: Modified Concrete Overlays
16 Feet
15’
cantilever
52 Feet
curb - curb
I-90 Denny Creek Bridge
Transverse Post Tensioning
3.5” below top of deck

## Slide 47: Modified Concrete Overlays
Deck Patching / Spalls
1,871 SF (1.0%)
NBI Deck – 6
“Fair” Condition
I-90 Denny Creek Bridge

## Slide 48: Modified Concrete Overlays
I-90 Denny Creek Bridge
Bridge Deck Rehab
Hydromill and Concrete Overlay
2017

## Slide 49: Modified Concrete Overlays
I-90 Denny Creek Bridge
Bridge Deck Rehab
Hydromill and Concrete Overlay
2017

## Slide 50: Modified Concrete Overlays
I-90 Denny Creek Bridge
Bridge Deck Rehab
Hydromill and Concrete Overlay
2017

## Slide 51: Modified Concrete Overlays
I-90 Denny Creek Bridge

## Slide 52
Chart: 
| Bare Conc | Bare Conc-ECR | Conc Overlays | Asphalt | Polyester | Polymer
Deck Area | 8845361 | 13219991 | 13278192 | 8521431 | 742661 | 388783
 | 816351


(19.3%)
(28.9%)
(1.6%)
(30.8%)
(18.6%)
(0.8%)
792
589
564
23
1030
21
Washington State’s Concrete Bridge Deck Program
21
3,039 Bridges with Concrete Decks
45.8 million SF deck area
(2nd and 3rd Gen)
8.8M SF
13.2M SF
14M SF
8.5M SF

## Slide 53: Asphalt Paving Train

## Slide 54: Paving Equipment Loads
Dump Truck: 40 Ton 3 axles
Planer: 45 Ton 2 tracks
Material Transfer: 70 Ton 2 axles
Paver: 40 Ton 1 track
Compactor: 15T+15T Vib. 2 axles
  Dump trucks and pup are legal loads.
  Paving Equipment does not have Legal Axles.
Posted bridges will limit operations.

## Slide 56: Asphalt Removal – Tacoma Narrows Bridge
Older bridge
Built - 1949

## Slide 57: Asphalt Removal – Tacoma Narrows Bridge
50k
40k
29k
29k
34k
52k
40k
40k
25 ft
25 ft
17 ft
52k

## Slide 58: Asphalt Removal by Rotomill

## Slide 59: Standard Rotary Mill Head
5/8” Planer Head Tooth Spacing.
Most common method used to remove asphalt.
New spec allows for Partial Removal only.
Edges will break off Typical Surface – 5/8” Spacing Replacing Teeth
Asphalt Removal – Milling Machine

## Slide 60: Asphalt Removal – Milling Machine
Rotary milling has the risk of damaging the concrete deck.

## Slide 61: Asphalt Removal - Scraping
Scraping with Loader, Grader, Bob Cat
Backhoe with a welded bar on the bucket
Scraping to remove ACP Required when:
Bridges over 100 feet in length
Bridges with integral bridge decks

## Slide 62: Asphalt with Membrane Overlay
Open – Sept 1978 (40 yrs)
SR397 – Columbia R
Ed Hendler Bridge
Located near Pasco/Kennewick
1st Major Cable Stayed Bridge in USA
Length – 2,503 feet
Max Span – 981 feet
Deck Width – 60 feet
Original Cost - $30M
Replacement Cost - $120M+

## Slide 63
SR397 – Columbia R
Ed Hendler Bridge
Located near Pasco/Kennewick

## Slide 64: Asphalt with Membrane Overlay
Asphalt History
1978 - 1st ACP Overlay
1986 – Mill Fill 0.15’
1998 – New ACP w/Memb
2017 – New ACP w/Memb
SR397 – Columbia R
Ed Hendler Bridge
ADT – 16,129

## Slide 65: Asphalt with Membrane Overlay
SR397 – Columbia R
Ed Hendler Bridge
8” Top Deck
2” Conc Cover
Standard Rebar
Each Segment is 27 x 80 feet
Weight - 300 tons

## Slide 66: Asphalt with Membrane Overlay
SR397 – Columbia R
Ed Hendler Bridge
Scraping to remove Asphalt

## Slide 67: Asphalt with Membrane Overlay
SR397 – Columbia R
Ed Hendler Bridge

## Slide 68: Asphalt with Membrane Overlay
SR397 – Columbia R
Ed Hendler Bridge
Applying Membrane

## Slide 69
Chart: 
| Bare Conc | Bare Conc-ECR | Conc Overlays | Asphalt | Polyester | Polymer
Deck Area | 8845361 | 13219991 | 13278192 | 8521431 | 742661 | 388783
 | 816351


(19.3%)
(28.9%)
(1.6%)
(30.8%)
(18.6%)
(0.8%)
792
589
564
23
1030
21
Washington State’s Concrete Bridge Deck Program
21
3,039 Bridges with Concrete Decks
45.8 million SF deck area
(2nd and 3rd Gen)
8.8M SF
13.2M SF
14M SF
8.5M SF

## Slide 70: Polyester Concrete Overlays
Chart: 
| Fair | Good | Poor
Deck Area | 533471 | 277748 | 26573
Ave Age – 21yrs
Oldest – 29yrs
8 bridges
> 25 yrs
23 Bridges
838K SF
4 Bridges
533.5K SF
(63.7%)
Fair
Good
16 Bridges
278K SF
(33.1%)
3 Bridges
26.5K SF
(3.2%)
Expected Service Life
25+ years
Total Project Cost
$100 - $125 / SF

## Slide 71: Polyester Concrete Overlays
I-5 NB Viaduct
Located in Seattle
Bridge Built – 1966
Polyester applied - 2007
ADT – 90,000

## Slide 72: Polyester Concrete Overlays
Interstate 90
2017

## Slide 73
Chart: 
| Bare Conc | Bare Conc-ECR | Conc Overlays | Asphalt | Polyester | Polymer
Deck Area | 8845361 | 13219991 | 13278192 | 8521431 | 742661 | 388783
 | 816351


(19.3%)
(28.9%)
(1.6%)
(30.8%)
(18.6%)
(0.8%)
792
589
564
23
1030
21
Washington State’s Concrete Bridge Deck Program
21
3,039 Bridges with Concrete Decks
45.8 million SF deck area
(2nd and 3rd Gen)
8.8M SF
13.2M SF
14M SF
8.5M SF

## Slide 74: Thin Polymer Overlays
US101 Chehalis River Bridge

## Slide 75
Summary of WSDOT Bridge Deck Rehabilitation Options
Deck Protection | Criteria for use
Epoxy Coated Rebar | All New Bridges
Asphalt / Membrane | Exist Asphalt / Deck in Good Cond
Modified Conc Overlay | Br Decks with > 2% Patching
Polyester Overlay | Br Decks with < 2% Patching
Polymer Overlay | Movable Bridges

## Slide 76
How do we Measure Success?
WSDOT’s Concrete Bridge Deck
Preservation Program

## Slide 77
WSDOT Bridge Deck Replacements
16 bridges (588,536 sq ft) [1.5% of total Statewide Deck Area]
Br Num | Yr | Length
395/40 | 1986 | 2,451
12/512N | 1987 | 1,270
82/280S | 1988 | 1,471
395/16 | 1988 | 72
240/32W | 1989 | 244
281/1 | 1990 | 196
9/130 | 1991 | 344
529/10E | 1994 | 1,544
397/10 | 1995 | 261
509/101 | 1995 | 562
509/103 | 1995 | 264
433/1 | 2004 | 5,478
97/1 | 2009 | 2,567
10/143 | 2012 | 430
5/670W | 2014 | 859
82/280S | 2018 | 1,920

## Slide 78: WSDOT Br Deck Preservation Savings
Epoxy Coated Rebar - $1/SF
ACP w/membr - $20/SF
Conc Overlay - $80/SF
Polyester Overlay - $120/SF
Replace Deck - $250/SF
Replace Bridge - $800/SF
14M SF / 2 x $170/SF = $1.2 Billion Savings (over 35 yrs)

## Slide 79
Questions?
WSDOT’s Concrete Bridge Deck Preservation Program